LIST OF FIGURES
[image: image1.jpg]Intensity (a.u)

25

20

—
D

—_—
)

O-olivine
M-magnetite
Py-pyroxene
G-granate

20()




Figure 1. XRD pattern for the copper slag sample

[image: image2.png]



Figure 2. Photomicrographs of the smelting slag (reflected light, air, II N): a – ferrite dendrites in the fayalite structure, b – magnetite shaped as a cube in the fayalite structure, c – chalcopyrite in the fayalite structure, d – copper matte in the fayalite structure. 

[image: image3.png]o (o2}
o o

n
o

Metal dissolution, %
N w
o o

-
o

0 bm:
0 15 30 45 60 75 90 105 120

Dissolution time, min




Figure 3. Copper and iron extractions from the slag as a function of time at different initial hydrochloric acid concentrations
[image: image4.png]etal dissolution, %

M
8

60 75 90
Dissolution time, min

105

120




Figure 4. Copper and iron extractions from the slag as a function of time at different initial hydrogen peroxide concentrations (1 M HCl, 350 min-1)
[image: image5.jpg]Intensity (a.u)

O-olivine
M-magnetite
Py-pyroxene
G-granate





Figure 5. XRD pattern for the leach residue (1 M HCl, 2 M H2O2)
[image: image6.png]Metal dissolution, %

o)
f=1

o
=]

N
o

w
o

N
o

L .
90 105 120
Dissolution time, min





Figure 6. Copper and iron extractions from the slag with and without stirring
[image: image7.png]Metal dissolution, %

s A
45 60 75 90
Dissolution time, min

1 L
105 120




Figure 7. Copper and iron extractions from the slag as a function of time at different temperatures
[image: image8.png]Metal dissolution, %

60

solid : liquid

<7 2MH0,
M HCI

L L L L L
40 60 80 100 120
Dissolution time, min





Figure 8. Copper and iron extractions from the slag as a function of time at different solid/liquid ratios
[image: image9.png]70

60

50

Temperature, °C
w
o

H0, Slag

-®--3M 5.00g
—8—2M 5.00g
—A—2M 10.00g

—¥—2M 15.00g
. 2M 20.00;

[HCII=1.0M
350 i

L L L L 1 1

4
30 45 60 75 90 105 120
Dissolution time, min





Figure 9. Suspension temperatures as a function of time at different solid/liquid ratios
[image: image10.png]Metal dissolution, %

~
o

(o2}
o

o
o

N
o

w
o

N
o

10

—— Adding lixiviant from an
automatic burette
lixiviant in portions

0 15 30 45 60 75 90 105 120 135
Dissolution time, min




Figure 10. Effect of the mode of lixiviant addition on metal dissolution from the slag 
