List of all Figures:

Fig. 1 Cover forgings: a) photo of forging after finishing forging, b) “hot” forgings after the forging and trimming process, placed on a conveyor belt leading to controlled cooling

Fig. 2 Massey press with pressing force 18 MN; a) photo of entire machine, b) view of cover forging tool mounted on press

Fig. 3 Tool set in II operation of roughing (preliminary forging)

Fig. 4 List of analyzed forging process parameters

Fig. 5 Macro view of the face part of analyzed tools after manufacturing of approx. 4000 forgings: a) after nitriding, b) after regenerative hardfacing, c) with Cr/CrN layer and d) with AlCrTiN layer

Fig. 6 Comparison of changes in tool geometry after manufacturing of 4000 forgings based on scanning results: a) nitrided, b) hardfaced, c) Cr/CrN, d) AlCrTiN

Fig. 7 SEM and light microscopy investigations of the surface layer of the tool with Cr/CrN coating in selected subareas: a) division of tool into elementary areas, b), c), d), f) photographs of microstructure in selected areas of the tool

Fig. 8 HV microhardness distribution on the cross-section of tools: a) in area R2,   
b) in area P2

Fig. 9 Contact normal stress [MPa] on the contact surface of the filler and the forging: general view (left) and longitudinal section (right), b) temperature of the filler in the lower dead centre of the press slide: 3D image (left) and longitudinal view (right)

Fig. 10 General scheme of the adopted neural network

Fig. **11** Correlation chart prepared on the basis of the results of observation and test results generated based on the MLP 5-13-1 network model

Fig. 12 Correlation charts prepared on the basis of results of observations and results generated on the basis of developed network models: a) ANN-1 (nitriding layer), b) ANN-2 (repair welding layer), c) ANN-3 (GN/CrN), d) ANN-4 (GN/AlCrTiN layer

Fig. 13 Determination of wear (geometrical loss) for nitrided layer, a) T=500, path of friction=1, b) T=500, path of friction 10 mm

Fig. 14 Determination of wear (geometrical loss) for hardfaced layer, a) T=500, path of friction=1, b) T=500, path of friction 10 mm

Fig. 15 Determination of wear (geometrical loss) for GN/CrN layer, a) T=500, path of friction=1, b) T=500, path of friction 10 mm

Fig. 16 Determination of wear (geometrical loss) for GN/AlCrTiN layer, a) T=500, path of friction=1, b) T=500, path of friction 10 mm

Fig. 17 Determination of wear (geometrical loss) for nitrided layer, a) T=500, pressure=500[MPa] , b) T=500, pressure 700 [MPa]

Fig. 18 Determination of wear (geometrical loss) for hardfaced layer, a) T=500, pressure=500[MPa] , b) T=500, pressure 700 [MPa]

Fig. 19 Determination of wear (geometrical loss) for GN/CrN layer, a) T=500, pressure=500[MPa] , b) T=500, pressure 700 [MPa]

Fig. 20 Determination of wear (geometrical loss) for GN/AlCrTiN layer, a) T=500, pressure=500[MPa], b) T=500, pressure 700 [MPa]