Table 1 Test conditions (temperature and time of exposure at a specific temperature) of the samples investigated.

| Sample name | Deposition process | Base material | Test temperature /°C | Time test /h |
| --- | --- | --- | --- | --- |
| MR7Xh | LPPS | René80 | 700 | 300-500-1000-2000-3000-5000 |
| MR8Xh | LPPS | René80 | 800 | 300-500-1000-3000 |
| MR9Xh | LPPS | René80 | 900 | 300-500-1000-2000-3000-5000 |

*The sample name contains the experimental information: M=MCrAlY on Renè80; 7, 8, 9 = test temperature 700, 800 ,900; Xh = hours  of time exposure.

LPPS = Low Pressure Plasma Spray