Table 1  Characteristics of raw material powders applied in the TLPS process.

| Powder | Diameter /m | Chemical composition /at.% | Melting temperature /°C |
| --- | --- | --- | --- |
| Fine Ag | 5 - 20 | 99.99 Ag | 961.9 |
| Medium Ag | 20 - 25 |  |  |
| Coarse Ag | 25 - 53 |  |  |
| Sn-17Bi-1Ag | < 53 | 82Sn-17Bi-1Ag | 140 / 200 |

Table 2  Blend ratio and substantial composition of TLPS samples.

| Sample | Blend ratio /g | Substantial chemical composition /at.% |
| --- | --- | --- |
|  | Ag | Sn-17Bi-1Ag | Ag | Sn | Bi | Ag/Sn |
| #1 | 0.137 | 0.063 | 74 | 22 | 4 | 3.36 |
| #2 | 0.134 | 0.066 | 71 | 24 | 5 | 2.96 |