Directional solidification of Zn–Al–Cu eutectic alloy by the vertical Bridgman method

- The Zn–7wt.%Al–4wt.%Cu eutectic alloy were directionally solidified upward with different growth rates (V=11.62–230.77 m/s) at a constant temperature gradient (G=7.17 K/mm) and with different temperature gradients (G=7.17–11.04 K/mm) at a constant growth rate (V=11.62 m/s) by a Bridgman furnace.

- The microstructures were observed to be lamellae of Zn, Al and broken lamellae CuZn4 phases from quenched samples.

- The eutectic spacing, microhardness and ultimate tensile strength values for directional solidified Zn–7wt.%Al–4wt.%Cu eutectic alloy have been measured.

- The relationships among eutectic spacing, microhardness, ultimate tensile strength and growth rates/temperature gradient were obtained by regression analysis.